NMR relaxometry: correlations with SB block copolymer topologies and mechanical properties in blends with GPPS
Diffusion
challenges
in (chemical)
industries
Nikolaus Nestle
BASF Aktiengesellschaft
Polymer Physics
Ludwigshafen, Germany
Diffusion Fundamentals II
27.08.07
L'Aquila, Abruzzi, Italia

---
Introduction: SBS block copolymers Immiscible polymers chained together. Microphase separation. Phase diagram and properties.
The many contexts of
diffusion...
...@ DiffuFu-II:
Talks Cavalli-Sforza, Vogl
Poster B9 (Fujie, Odagaki)
...@ in economic life: ...

---
Limiting the topic a bit...
... Fickian and near-Fickian diffusion
of molecules and/or energy

---
Outline
Scaling behaviour of diffusion effects
Diffusion as a challenge:
Diffusion of heat
Diffusion of reactants
Diffusion in multicomponent
 materials and finished goods
Diffusion as a friend: controlled release
Going micro and nano: approaching the apparent dwarf

---
Scaling behaviour of
diffusion effects
Macroworld
experience:
Diffusion is
slow.
Typical
example:
a real
Saxonian
„Semester-
uhr“
(„term
clock“)

---
Scaling behaviour of
diffusion effects
Macroworld
experience:
Diffusion is
slow.
Typical
example:
a real
Saxonian
„Semester-
uhr“
(„term
clock“)
Nevertheless:
sufficient change
to observe during
first hour of the
experiment.

---
Scaling behaviour of
diffusion effects
Macroworld
experience:
Diffusion is
slow.
Typical
example:
a real
Saxonian
„Semester-
uhr“
(„term
clock“)
Nevertheless:
sufficient change
to observe during
first hour of the
experiment.
Non-linear time
behaviour of diffusion
... taking a closer look at the short-
time behaviour...

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:
density-driven flow
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:	Suppression of convection
density-driven flow	by xanthan
Xanthan gum, 0,5 % w/v
dissolved in water
(no major effect on diffusion)
Water
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:	Suppression of convection
density-driven flow	by xanthan
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:	Suppression of convection
density-driven flow	by xanthan
Convection cells,
„interference“
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:	Suppression of convection
density-driven flow	by xanthan
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:	Suppression of convection
density-driven flow	by xanthan
Diffuse concentration
profiles, no „interference“
KMnO4

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Dominating effect:	Suppression of convection
density-driven flow	by xanthan
Seemingly
constant
supply of
dissolved
KMnO4
Diffuse concentration
profiles, no „interference“
KMnO4
Propagation
of eosin
slows
down with
time

---
Scaling behaviour of
diffusion effects
Dissolution of coloured ions: KMnO4 and eosin
Diffusion through thin
stagnant layer at crystal-
water interface allows
fast mass transport into
region of convective flow.
Fast convection
on macroscale
is fed by fast
diffusion on micro-
scale.
Diffusion: really slow?
Diffusion limited interface layer

---
Scaling behaviour of
diffusion effects
       Fick's first law	Fourier's law	Fouriersches Gesetz
„Large“
reservoirs
Stationary
profile of
c or T in wall
Diffusive
current through
wall:
c1 c2
c1 c2
T1 T2
T1 T2
l
l
j_D=-D{c_1 - c_2}over{l} newline {j_D}=-D{dc}over{dx}
j_Q=-{%lambda}{T_1 - T_2}over{l} newline {j_Q}=-{%lambda}{dT}over{dx}

---
Scaling behaviour of
diffusion effects
       Fick's first law	Fourier's law	Fouriersches Gesetz
„Large“
reservoirs
Stationary
profile of
c or T in wall
Diffusive
current through
wall:
c1 c2
c1 c2
Everything still seems linear ...
... however: What happens for
instationary situations?
T1 T2
T1 T2
l
l
j_D=-D{c_1 - c_2}over{l} newline {j_D}=-D{dc}over{dx}
j_Q=-{%lambda}{T_1 - T_2}over{l} newline {j_Q}=-{%lambda}{dT}over{dx}

---
Scaling behaviour of
diffusion effects
Example: instationary heat diffusion:
Heat current produces change in
inner energy, i.e. heating of volume
element:
dU=(j_Q(x)-j_Q(x+dx)A)dt
dU=Cdm{dT}over{dt}dt=C{%rho}dV{dT}over{dt}dt=C{%rho}Adx{dT}over{dt}dt

---
Scaling behaviour of
diffusion effects
Example: instationary heat diffusion:
Heat current produces change in
inner energy, i.e. heating of volume
element:
Comparing the expressions leads to
dU=(j_Q(x)-j_Q(x+dx)A)dt
dU=Cdm{dT}over{dt}dt=C{%rho}dV{dT}over{dt}dt=C{%rho}Adx{dT}over{dt}dt
C{%rho}Adx{dT}over{dt}dt=(j_Q(x)-j_Q(x+dx))Adt
C{%rho}{dT}over{dt}dx=(j_Q(x)-j_Q(x+dx))=-dj_Q(x)

---
Scaling behaviour of
diffusion effects
Example: instationary heat diffusion:
Heat current produces change in
inner energy, i.e. heating of volume
element:
Comparing the expressions leads to
dU=(j_Q(x)-j_Q(x+dx)A)dt
dU=Cdm{dT}over{dt}dt=C{%rho}dV{dT}over{dt}dt=C{%rho}Adx{dT}over{dt}dt
C{%rho}Adx{dT}over{dt}dt=(j_Q(x)-j_Q(x+dx))Adt
{j_Q}=-{%lambda}{dT}over{dx}
C{%rho}{dT}over{dt}dx=(j_Q(x)-j_Q(x+dx))=-dj_Q(x)
C{%rho}{dT}over{dt}=-{{dj_Q(x)}over{dx}}={%lambda}{d^{2}T}over{dx^2}
Fick's second law of heat diffusion

---
Scaling behaviour of
diffusion effects
Example: instationary heat diffusion:
Heat current produces change in
inner energy, i.e. heating of volume
element:
Comparing the expressions leads to
dU=(j_Q(x)-j_Q(x+dx)A)dt
dU=Cdm{dT}over{dt}dt=C{%rho}dV{dT}over{dt}dt=C{%rho}Adx{dT}over{dt}dt
C{%rho}Adx{dT}over{dt}dt=(j_Q(x)-j_Q(x+dx))Adt
{j_Q}=-{%lambda}{dT}over{dx}
C{%rho}{dT}over{dt}dx=(j_Q(x)-j_Q(x+dx))=-dj_Q(x)
{dc}over{dt}=D{d^{2}c}over{dx^2}
C{%rho}{dT}over{dt}=-{{dj_Q(x)}over{dx}}={%lambda}{d^{2}T}over{dx^2}
Fick's second law of
(matter) diffusion
Fick's second law of heat diffusion

---
Scaling behaviour of
diffusion effects
Solution of diffusion equation for d-shaped disturbance (1D):
c(x,t)={C_o}over{2{sqrt{{%pi}Dt}}}exp(-{x^2}over{4Dt})
Mean diffusive shift:
s_{D,1D}=sqrt{{}<{}x^2{}>{}}=sqrt{2Dt}

---
Scaling behaviour of
diffusion effects
Solution of diffusion equation for d-shaped disturbance (1D):
into a 3D medium
c(x,t)={C_o}over{2{sqrt{{%pi}Dt}}}exp(-{x^2}over{4Dt})
Mean diffusive shift:
s_{D,1D}=sqrt{{}<{}x^2{}>{}}=sqrt{2Dt}

---
Scaling behaviour of
diffusion effects
Solution of diffusion equation for d-shaped disturbance (1D):
Diffusion from a line source
into a 3D medium
c(x,t)={C_o}over{2{sqrt{{%pi}Dt}}}exp(-{x^2}over{4Dt})
Mean diffusive shift:
s_{D,1D}=sqrt{{}<{}x^2{}>{}}=sqrt{2Dt}
c(x,t)={M_o}over{4{%pi}Dt}exp(-{x^2}over{4Dt})

---
Scaling behaviour of
diffusion effects
Solution of diffusion equation for d-shaped disturbance (1D):
Diffusion from a line source
or a point source
into a 3D medium
c(x,t)={C_o}over{2{sqrt{{%pi}Dt}}}exp(-{x^2}over{4Dt})
Mean diffusive shift:
s_{D,1D}=sqrt{{}<{}x^2{}>{}}=sqrt{2Dt}
c(x,t)={M_o}over{4{%pi}Dt}exp(-{x^2}over{4Dt})
c(x,t)={M_o}over{8{(sqrt{{%pi}Dt})^3}}exp(-{x^2}over{4Dt})

---
Scaling behaviour of
diffusion effects
Solution of diffusion equation for d-shaped disturbance (1D):
Diffusion from a line source
or a point source
into a 3D medium
c(x,t)={C_o}over{2{sqrt{{%pi}Dt}}}exp(-{x^2}over{4Dt})
Mean diffusive shift:
s_{D,1D}=sqrt{{}<{}x^2{}>{}}=sqrt{2Dt}
Different normalization
factors due to geometry:
Faster depletion of con-
centration in center due
to growing volume
elements for cyclindrical
and spherical geometry.
c(x,t)={M_o}over{4{%pi}Dt}exp(-{x^2}over{4Dt})
c(x,t)={M_o}over{8{(sqrt{{%pi}Dt})^3}}exp(-{x^2}over{4Dt})

---
Scaling behaviour of
diffusion effects
More realistic scenarioes: semiinfinite media and finite sheets
{dT}over{dt}={%lambda}over{C{%rho}}{d^{2}T}over{dx^2}={%alpha}{d^{2}T}over{dx^2}
{%alpha}={%lambda}over{C{%rho}}
Heat diffusion coefficient
l l

---
Scaling behaviour of
diffusion effects
More realistic scenarioes: semiinfinite media and finite sheets
{dT}over{dt}={%lambda}over{C{%rho}}{d^{2}T}over{dx^2}={%alpha}{d^{2}T}over{dx^2}
{%alpha}={%lambda}over{C{%rho}}
Heat diffusion coefficient
l l
T(x,t) = {1 over 2}T_{o}erfc({x}over{2 sqrt{{%alpha}t}})
T(x,0) T(x,t)

---
Scaling behaviour of
diffusion effects
More realistic scenarioes: semiinfinite media and finite sheets
{dT}over{dt}={%lambda}over{C{%rho}}{d^{2}T}over{dx^2}={%alpha}{d^{2}T}over{dx^2}
{%alpha}={%lambda}over{C{%rho}}
Heat diffusion coefficient
l l
T(x,t) = {1 over 2}T_{o}erfc({x}over{2 sqrt{{%alpha}t}})
T(x,0) T(x,t)
T(x,t) = {1 over 2}T_{o}[erf({h-x}over{2 sqrt{{%alpha}t}})-erf({h+x}over{2 sqrt{{%alpha}t}}) ]
T(x,0) T(x,t)
-h h

---
Scaling behaviour of
diffusion effects
More realistic scenarioes: semiinfinite media and finite sheets
{dT}over{dt}={%lambda}over{C{%rho}}{d^{2}T}over{dx^2}={%alpha}{d^{2}T}over{dx^2}
{%alpha}={%lambda}over{C{%rho}}
Heat diffusion coefficient
l prop sqrt{{%alpha}t}
l l
Relevant charac-
teristic lenght
scale for all
diffusion processes
T(x,t) = {1 over 2}T_{o}erfc({x}over{2 sqrt{{%alpha}t}})
T(x,0) T(x,t)
T(x,t) = {1 over 2}T_{o}[erf({h-x}over{2 sqrt{{%alpha}t}})-erf({h+x}over{2 sqrt{{%alpha}t}}) ]
T(x,0) T(x,t)
-h h

---
Scaling behaviour of
diffusion effects
v_D={{s_D}}over{t_s}={s_D}over{{{s_D}^2}over{2D}}={2D}over{{s_D}}
„Velocity“ of diffusive transport processes:
Inversely proportional to diffusion length!

---
Scaling behaviour of
diffusion effects
v_D={{s_D}}over{t_s}={s_D}over{{{s_D}^2}over{2D}}={2D}over{{s_D}}
„Velocity“ of diffusive transport processes:
Inversely proportional to diffusion length!
Ratio of diffusive velocity to characteristic velocity in system:
Péclet number
{v_{Char}}over{v_D}={{s_D}v_{Char}}over{2D}
nitalic{bold{Pe}}={{L_{Char}}v_{Char}}over{D}

---
Scaling behaviour of
diffusion effects
v_D={{s_D}}over{t_s}={s_D}over{{{s_D}^2}over{2D}}={2D}over{{s_D}}
„Velocity“ of diffusive transport processes:
Inversely proportional to diffusion length!
Ratio of diffusive velocity to characteristic velocity in system:
Péclet number
        axial	and radial
{v_{Char}}over{v_D}={{s_D}v_{Char}}over{2D}
nitalic{bold{Pe}}={{L_{Char}}v_{Char}}over{D}

---
Diffusion as a challenge:
Heat
Heating extended objects
e.g. baking
Chapati
almost homogeneous
baking time
< 1min
European-
style bread
obviously inhomogeneous
baking time
> 1 h

---
Diffusion as a challenge:
Heat
Heating extended objects
e.g. baking
Chapati
almost homogeneous
baking time
< 1min
European-
style bread
obviously inhomogeneous
baking time
> 1 h
Heating up extended objects: intrinsically slow
(time- and energy consuming)
Speeding up:
Increased temperature gradient
Optimized heat transfer (convection)
Better alternative: avoid (i.e. reduce object size)
Benefits of slow heat transfer:
No thermal damage to interior in short high-temperature
treatment of outer surfaces (e.g. „Baked Alaska“)

---
Diffusion as a challenge:
Heat
Self-heating systems

---
Diffusion as a challenge:
Heat
Self-heating systems
Substantially higher temperatures
in extended objects (e.g. over
80 °C in massive concrete
structures vs. almost neglegible
heating in slender structures)

---
Diffusion as a challenge:
Heat
Self-heating systems
Substantially higher temperatures
in extended objects (e.g. over
80 °C in massive concrete
structures vs. almost neglegible
heating in slender structures)
Especially problematic for reactions
with positive temperature coefficient
Major danger in scale-up of
reactions (power excursions!)
Countermeasures: keep S/V
constant, increase stirring to
achieve better heat exchange,
active cooling

---
Diffusion as a challenge:
Heat
Heat-diffusion in buildings
      Nordic	Alpine
   Similar static heat conduction through walls
Low heat capacity	High heat capacity

---
Diffusion as a challenge:
Heat
Calderone Glacier @ Gran Sasso
25/08/07

---
Diffusion as a challenge
reactants
Traditional tanks and reactors:
Large Péclet numbers
Exceptions:
Heat exchangers
Intraparticle processes

---
Diffusion as a challenge
reactants
Traditional tanks and reactors:
Large Péclet numbers
Active mixing
processes needed
In low viscosity systems:
induce turbulence
Shorter length scales
for diffusive mixing
Smaller Pe

---
Diffusion as a challenge
reactants
Traditional tanks and reactors:
Large Péclet numbers
Exceptions:
Heat exchangers
Intraparticle processes
Active mixing
processes needed
In low viscosity systems:
induce turbulence
Shorter length scales
for diffusive mixing
Smaller Pe
High viscosity systems
Thorough mixing
 increasingly difficult
Typically lower D, too

---
Diffusion as a challenge
reactants
Polymerization reactions: especially strong increase in viscosity
due to entanglement effects.
Degree of polymerization
Polymer concentration
(solution processes)
 yield!
Branching and crosslinks

---
Diffusion as a challenge
reactants
Polymerization reactions: especially strong increase in viscosity
due to entanglement effects.
Degree of polymerization
Polymer concentration
(solution processes)
 yield!
Branching and crosslinks
Residual monomers
Plasticizers

---
Diffusion as a challenge
reactants
Polymerization reactions: especially strong increase in viscosity
due to entanglement effects.
Degree of polymerization
Polymer concentration
(solution processes)
 yield!
Branching and crosslinks
Temperature
heating energy!
decomposition!
Residual monomers
Plasticizers

---
Diffusion as a challenge
reactants
Polymerization reactions: especially strong increase in viscosity
due to entanglement effects.
Degree of polymerization
Polymer concentration
(solution processes)
 yield!
Branching and crosslinks
Temperature
heating energy!
decomposition!
Residual monomers
Plasticizers
More polymer dynamics
tomorrow: Talks Richter
and Sarti

---
Diffusion as a challenge
reactants
Alternative approach to polymerizations: emulsion polymerization
Especially attractive for production
of cross-linked polymers
Diffusive transport only at length
scale of droplets or micelles
Low-viscosity convection in conti-
nous liquid phase

---
Diffusion as a challenge
reactants
Alternative approach to polymerizations: emulsion polymerization
Especially attractive for production
of cross-linked polymers
Diffusive transport only at length
scale of droplets or micelles
Low-viscosity convection in conti-
nous liquid phase
Different modes of operation
depending on distribution of
monomers and starters
Surfactant material needed
Most typical case: oil-in water
emulsions
Monodisperse particles from
ordered micellar phases

---
Diffusion as a challenge
reactants
Cement hydration:
Dissolution of suspended
clinker grains	Repreciptation of CSH phases
Dissolution of unreacted
cement clinker increasingly
impeded by CSH diffusion barrier
Delayed hydration
poor use of clinker

---
Diffusion as a challenge
reactants
Poster C03 Bordallo et al. :
water in CSH phases
Cement hydration:
Dissolution of suspended
clinker grains	Repreciptation of CSH phases
Dissolution of unreacted
cement clinker increasingly
impeded by CSH diffusion barrier
Delayed hydration
poor use of clinker

---
Diffusion as a challenge
reactants
Enhanced hydration in the presence of microfillers
Inert microfillers
Cement hydration kinetics studied by TD-NMR
1/T1 essentially proportional to S/V inside cement stone matrix

---
Diffusion as a challenge
reactants
Enhanced hydration in the presence of microfillers
TiO2
Cement hydration kinetics studied by TD-NMR
1/T1 essentially proportional to S/V inside cement stone matrix

---
Diffusion as a challenge
reactants
Enhanced hydration in the presence of microfillers
Accelerated hydration desirable for
enabling faster construction.
Favourable permeability properties
due to denser pore system.
TiO2
Cement hydration kinetics studied by TD-NMR
1/T1 essentially proportional to S/V inside cement stone matrix

---
Diffusion as a challenge
composite products
T
Polymer 1 w/o plasticizer
Polymer 2 w plasticizer

---
Diffusion as a challenge
composite products
T
Polymer 1 w/o plasticizer
Polymer 2 w plasticizer
Possible adverse
effects of plasticizer

---
Diffusion as a challenge
composite products
T
Polymer 1 w/o plasticizer
Polymer 2 w plasticizer
Possible adverse
effects of plasticizer
Degradadion due to
loss of pasticizer

---
Diffusion as a challenge
composite products
T
Polymer 1 w/o plasticizer
Polymer 2 w plasticizer
Possible adverse
effects of plasticizer
Risk of
delamination
Degradadion due to
loss of pasticizer

---
Diffusion as a challenge
composite products
Parameters affecting diffusion effects
in composite materials
Distribution coefficient between two layers
Miscibility (possibly temperature effects)
Diffusion coefficient
Measures against diffusion
Reduction of diffusion coefficient
Introduction of barriers
T
Polymer 1 w/o plasticizer
Polymer 2 w plasticizer
Possible adverse
effects of plasticizer
Degradadion due to
loss of pasticizer

---
Diffusion as a challenge
composite products
Parameters affecting diffusion effects
in composite materials
Distribution coefficient between two layers
Miscibility (possibly temperature effects)
Diffusion coefficient
Measures against diffusion
Reduction of diffusion coefficient
Introduction of barriers
T
Polymer 1 w/o plasticizer
Polymer 2 w plasticizer
Possible adverse
effects of plasticizer
Risk of
delamination
Polymer 1 w/o plasticizer
Degradadion due to
loss of pasticizer
Polymer 2 w plasticizer

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Fresh

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Shelf-life
5 days later
Fresh

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Internal barriers: helping to maintain
local concentration gradients
Shelf-life

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Internal barriers: helping to maintain
local concentration gradients
Inside „homogeneous“ tissues:
Almost free diffusion (water and/or
vapour phase) in extracellular media
Possibly even faster transport
pathways due to capillary effects
Barrier action of cell walls much
weaker than outer barriers
Shelf-life

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Internal barriers: helping to maintain
local concentration gradients
Inside „homogeneous“ tissues:
Almost free diffusion (water and/or
vapour phase) in extracellular media
Possibly even faster transport
pathways due to capillary effects
Barrier action of cell walls much
weaker than outer barriers
Shelf-life
Drying

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Internal barriers: helping to maintain
local concentration gradients
Inside „homogeneous“ tissues:
Almost free diffusion (water and/or
vapour phase) in extracellular media
Possibly even faster transport
pathways due to capillary effects
Barrier action of cell walls much
weaker than outer barriers
Processing and spicing
marinated and pickled
foods
In absence of outer
barriers: 1 cm/day
Whole fruit with
intact skin (e.g.
olives): months

---
Diffusion as a challenge
food
Natural diffusion barriers
Outer skins: essential self-protection
systems of organisms against loss of
moisture and oxydation
Internal barriers: helping to maintain
local concentration gradients
Inside „homogeneous“ tissues:
Almost free diffusion (water and/or
vapour phase) in extracellular media
Possibly even faster transport
pathways due to capillary effects
Barrier action of cell walls much
weaker than outer barriers
Processing and spicing
marinated and pickled
foods
In absence of outer
barriers: 1 cm/day
Whole fruit with
intact skin (e.g.
olives): months
Mechanical or osmotic
disruption of barriers
before frying

---
Diffusion as a challenge
food composites
(Organic) chocolate after
a few weeks with occasional
heating episodes up to 30 °C
(i.e. in a kitchen without air
conditioning)
Macroscale demixing of solid
and liquid fat components and
diffusion to the surface
Similar effect in a Bacio with
internal (macroscopic) fat-fat
interfaces

---
Diffusion as a challenge
food composites
(Organic) chocolate after
a few weeks with occasional
heating episodes up to 30 °C
(i.e. in a kitchen without air
conditioning)
Macroscale demixing of solid
and liquid fat components and
diffusion to the surface
Similar effect in a Bacio with
internal (macroscopic) fat-fat
interfaces
Not just limited to food:
Similar high-temperature
effects in steel.
Posters B1, B2 Evteev et al.

---
Diffusion as a challenge
food composites
A sweets manu-
facturers' crunchy
trick to control
diffusive transport
between different
fat phases
Insert a hydrophilic
cracknel
capillary barrier
between the two
fatty layers

---
Diffusion as a friend:
controlled release
Active agent
Substrate	Target

---
Diffusion as a friend:
controlled release
Active agent dissolved in high concentration
Concentration difficult to maintain (e.g. washout,
degradation)
Side effects
Substrate	Target

---
Diffusion as a friend:
controlled release
Active agent dissolved in low concentration
Concentration difficult to maintain (e.g. washout,
degradation)
Less side effects
Substrate	Target

---
Diffusion as a friend:
controlled release
Constant supply of agent for dissolution:
Desired effect: maintainance of a low and effective
agent concentration for a long time
Substrate	Target

---
Diffusion as a friend:
controlled release
Constant supply of agent for dissolution:
Desired effect: maintainance of a low and effective
agent concentration for a long time
Substrate	Target

---
Diffusion as a friend:
controlled release
Constant supply of agent for dissolution:
Desired effect: maintainance of a low and effective
agent concentration for a long time
Substrate	Target

---
Diffusion as a friend:
controlled release
Constant supply of agent for dissolution:
Desired effect: maintainance of a low and effective
agent concentration for a long time
Remaining
challenges:
Time profile
of release
Delayed
onset of
action
Combination
of several
agents
Substrate	Target

---
Diffusion as a friend:
controlled release
Constant supply of agent for dissolution:
Desired effect: maintainance of a low and effective
agent concentration for a long time
Remaining
challenges:
Time profile
of release
Delayed
onset of
action
Combination
of several
agents
Substrate	Target
Related topic:
poster D3
Pilar et al.

---
Going micro and nano:
approaching the apparent dwarf
Washing out a blue colour
tracer (C.I. Basic Violet 3)
from a circular flat cell
10 mm

---
Going micro and nano:
approaching the apparent dwarf
Washing out a blue colour
tracer (C.I. Basic Violet 3)
from a circular flat cell
Context: Interplay
between diffusion and
relaxation in thin excited
slices
(A. Gädke and N.N., Diffusion
Fundamentals 3 38.1-38.12)
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 4.5 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 4.5 s of 10 ml/min
water flow.
10 mm
Almost no notable
decolouring of feed
line

---
Going micro and nano:
approaching the apparent dwarf
After 9 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 13.5 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 18 s of 10 ml/min
water flow.
10 mm
Almost complete
decolouring
of feed line

---
Going micro and nano:
approaching the apparent dwarf
After 22.5 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 27 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 31.5 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 36 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 40.5 s of 10 ml/min
water flow.
10 mm

---
Going micro and nano:
approaching the apparent dwarf
After 45 s of 10 ml/min
water flow.
10 mm
Almost no wash-out in region
outside of convection pathways
needs further flooding for several
minutes until substantial washout
occurs.

---
Going micro and nano:
approaching the apparent dwarf
After 45 s of 10 ml/min
water flow.
Is continous flooding really
necessary?
Saving solvent
More sustainable process?
Help by diffusion?
10 mm
Almost no wash-out in region
outside of convection pathways
needs further flooding for several
minutes until substantial washout
occurs.

---
Going micro and nano:
approaching the apparent dwarf
After waiting 3 min
10 mm
Diffusive broadening of remaining
(C.I. Basic Violet 3)

---
Going micro and nano:
approaching the apparent dwarf
After 15 s of subsequent
flooding
10 mm

---
Going micro and nano:
approaching the apparent dwarf
Example shows: clever division of work between flow and
diffusion helps saving resources
Heterogeneous catalysis
Adsorption and ion exchange	(Posters C4, C8,...)
Environmental remediation	(Talk Barker, Poster F4)
Chromatography	(Poster C11)
Lab on a chip
Living organisms	(Posters D6, D7)

---
Ringrazio tanto!
Stefano Brandani
Jörg Kärger
Roberto Volpe
Christian Chmelik
Anna Cicolani
Walter Heckmann
Achim Gädke